|  | Filter fleece – Technical Information |
| --- | --- |

| Filtervlies V… | Filtervlies PES-S FT… | Filtervlies PP-S… | Filtervlies D… |
| --- | --- | --- | --- |
| 100% Viscose binder solidified | 100% Polyester thermal solidified | 100% Polypropylene thermal solidified | 100% Polyester, very thin fibers needled and thermally solidified |
| Use in: Gravity band filter, compact band filter | Use in: Hydrostatic filter, inclined bed filter, pressure belt filter, vacuum belt filter, Achenbach plate filter | Use in: pressure belt filter | Use in: Hydrostatic filter, inclined bed filter, pressure belt filter, vacuum belt filter, Achenbach plate filter, compact band filter, large gravity band filter |
|  |  |  | Fleece has mounting direction: smooth side down |
| V 20 170 µ filtering / pore size 6500 l/m²/s throughput | PES-S FT 20 200 µ filtering / pore size 7500 l/m²/s throughput | PP-S 20 160 µ filtering / pore size 6200 l/m²/s throughput | D 50 HS 80 µ filtering / pore size 5600 l/m²/s throughput |
| V 30 110 µ filtering / pore size 5500 l/m²/s throughput | PES-S FT 30 180 µ filtering / pore size 5100 l/m²/s throughput | PP-S 30 130 µ filtering / pore size 4200 l/m²/s throughput | D 70 HS 70 µ filtering / pore size 4000 l/m²/s throughput |
| V 35 100 µ filtering / pore size 5000 l/m²/s throughput | PES-S FT 40 150 µ filtering / pore size 4000 l/m²/s throughput | PP-S 40 750 µ filtering / pore size 3600 l/m²/s throughput | D 100 HS 65 µ filtering / pore size 3500 l/m²/s throughput |
| V 40 90 µ filtering / pore size 4000 l/m²/s throughput | PES-S FT 50 130 µ filtering / pore size 3100 l/m²/s throughput | PP-S 50 60 µ filtering / pore size 2700 l/m²/s throughput | D 130 H 55 µ filtering / pore size 3200 l/m²/s throughput |
| V 50 80 µ filtering / pore size 3400 l/m²/s throughput | PES-S FT 60 100 µ filtering / pore size 2600 l/m²/s throughput |  | D 160 H ***hone quality*** 35 µ filtering / pore size 2200 l/m²/s throughput |
| V 60 70 µ filtering / pore size 2700 l/m²/s throughput | PES-S FT 70 80 µ filtering / pore size 2400 l/m²/s throughput | PP-S 70 50 µ filtering / pore size 1800 l/m²/s throughput |  |
|  | PES-S FT 100 40 µ filtering / pore size 1300 l/m²/s throughput | PP-S 100 40 µ filtering / pore size 1200 l/m²/s throughput |  |

Core diameter: 70mm